_____________________________________________________________________

Visco 2000

Classic Mineral Oil

_____________________________________________________________________________

Applications

| BP Visco 2000 is an SAE 15W-40 multigrade crankcase oil primarily intended for gasoline engines, but is equally suitable for many naturally aspirated and turbocharged diesel engines used in passenger cars. | . |
| --- | --- |

_____________________________________________________________________________

Main Benefits

| Stay in grade performance Higher viscosity provides proven engine protection |  |
| --- | --- |

_____________________________________________________________________________

Specifications

| The internationally-recognised standards that are used by manufacturers to specify oils for use in their engines, and which BP Visco 2000 meets or exceeds, include : - API SL/CF - ACEA A3/B3 | BP Visco 2000 meets the requirements of most major motor manufacturers of Europe, America and Japan. - VW 505 00 - MB 229.1 |
| --- | --- |

_____________________________________________________________________________

Storage

| All packages should be stored under cover. Where outside storage is unavoidable drums should be laid horizontally to avoid the possible ingress of water and | the obliteration of drum markings. Products should not be stored above 60°C, exposed to hot sun or freezing conditions. |
| --- | --- |

_____________________________________________________________________________

Health, Safety and Environment

| Health, safety and environmental information is provided for this product in the Materials Safety Data Sheet. This gives details of potential hazards, precautions and First Aid measures, together with environmental effects and disposal of used products. | BP p.l.c. or its subsidiaries will not accept liability if the product is used other than in the manner or with the precautions or for the purpose/s specified. Before the product is used other than as directed, advice should be obtained from the local BP office. |
| --- | --- |

_____________________________________________________________________________

_____________________________________________________________________

Visco 2000

Classic Mineral Oil

_____________________________________________________________________________

Typical Characteristics

_____________________________________________________________________________

|  | Test Methods | Units | Grade : |
| --- | --- | --- | --- |

_____________________________________________________________________________

SAE 15W-40

_____________________________________________________________________________

| Test | Method(s) | Unit | Typical |
| --- | --- | --- | --- |
| Density @ 15C, Relative | ASTM D4052 |  | 0.885 |
| Appearance | Visual |  | Clear & bright amber liquid |
| Viscosity, Kinematic 100C | ASTM D445 | mm²/s | 14.03 |
| Viscosity, Kinematic 40C | ASTM D445 | mm²/s | 107 |
| Viscosity Index | ASTM D2270 |  | 131 |
| Viscosity, CCS -20C (15W) | ASTM D5293 | cP | 6700 |
| Flash Point, PMCC | ASTM D93 | °C | 196 |
| Ash, Sulphated | ASTM D874 | % wt | 1 |
| Total Base Number, TBN | ASTM D2896 | mg KOH/g | 8 |

_____________________________________________________________________________

The above figures are typical of those obtained with normal production tolerance and do not constitute a specification.

| This Data Sheet and information it contains is considered to be accurate at the date of printing. No warranty or representation, expressed or implied, is made as to the accuracy or completeness of the data and information contained in this publication. | The Seller shall not be responsible for any loss or damage resulting from any hazards or risks identified in the data sheet and which are associated with petroleum products concerned (provided that this disclaimer shall not affect any statutory rights of the Buyer of the petroleum products concerned). |
| --- | --- |
| It is the User's obligation to evaluate and use products safely and within the scope advised in the data sheet and to comply with all applicable laws and regulations. No statement made in this publication shall be construed as a permission, recommendation or authorisation given or implied to practice any patented invention without a valid licence. |  |

_____________________________________________________________________________